## Slide 1
www.wasteeng.org
9th International Conference on Engineering for Waste and Biomass Valorisation
June 27-30, 2022
Copenhagen, Denmark
Experimental study of the use dredged sediments in a hydrocarbon matrix
Fouad BELAYALI, Walid MAHERZI, Nor-Edine ABRIAK, Mahfoud BENZERZOUR
logos
1. Univ. Lille, IMT Nord Europe, Univ. Artois, JUNIA, ULR 4515 - LGCgE, Laboratory of Civil Engineering and Geo-Environment, F-59000, Lille, France;
Notes: Good morning ladies and gentelmen
My name is Walid Mhaerzi, i am an assistant professor at IMT Nord Europe in France, i would like first to express my plaisir to particpate in this very interessting conference concerning waste and biomass valorisation
today i am gonna talk about the USE OF TERNARY BINDER BASED ON CLAYEY CALCINED SEDIMENTS FOR THE STABILIZATION OF MINERAL WASTE, it is a part of reaserch thesis of Selma BELLARA

## Slide 2
Results
04
Conclusions and perspectives
Background and study objectives
Materials and research methodology
03
02
01
Summary
2
Notes: This is the outline of the presentation
First i will begin by a background and study objectives
Followed by the research methodologie,
Experimental approach
And i will finish with some conclusions and future work

## Slide 3
3
In 2016, we produced 326 Mt of waste
224 Mt from the construction & public works sector
4,6 tonnes of waste per capita/year
Fortunately, some industries use secondary raw materials (alternative materials) in their activities: 66% for the paper industry, 58% for the glass industry, 50% for the steel industry and 6% for plastics and 27% for construction sector.
Waste production in France
Sources : Eurostat – Production de déchets des entreprises 2006 à 2016 ;
ADEME – Enquête Collecte 2015 ;
ADEME – Bilan du recyclage 2005-2014 ;
Background and study objectives

## Slide 4
Background and study objectives
4
Use & Needs of aggregates in France
321.5 Mt aggregates extracted from quarries
121.5 Mt aggregates from recycling
2.2 Mt imported from outside
6 tones per capita per year and 17 kg per capita per day
UNICEM - Union nationale des industries de carrières et des matériaux de construction 2018
Notes: On the other hand, Huge amounts of mineral waste are produced each year.
One such waste is dredged sediments:
The main water resource is based on the exploitation of hydraulic dams. Algeria has about 74 dams in service, the siltation rate of these dams was estimated about 65 million m3 in 2017 compared to 45 million cubic meters in 2006, a loss of 20% of their initial capacity.
Dredging operations are therefore essential in order to restore the initial water production capacity.
Blast furnace slag and marble waste are also another type of waste wich are found in abundant quantities in the East of Alegria

## Slide 5
5
5
Sediments are a fine particles (clays, silts) or coarse particles (sands), displaced and transported by climatic actions (wind, tides, ...) and human (development work, soil exploitation, ...).
Sediments are considered waste when they are extracted from water
Dredging sediments
Immersion
Storage
Valorisation
?
Background and study objectives
Notes: Turning now to the study methodology
a mix design was built for the optimization of ternary binders based on cement, GGBS and calcined sediments.
The Design expert software was used here to evaluate the effect of input parameters on the output parameters (wich is here the compressive strength of the mortar after 28 days).
The experimental design space obtained is shown in the figure. The red dots represents the proposed formulations.
11 mixtures were formulated with a water cement ratio of 0.5 and then tested for mechanical strength.
The most suitable regression model (quadratic regression ) was chosen for the prediction of compressive strengths.
The two formulations 80 Cement 10 Slag 10 Calcined Sediments and 50 Cement 35 Slag 15 Calcined Sediments were selected to validate the quadratic model

## Slide 6
6
Potential applications for the valorization of sediments in building materials
Sealing asphalt
Intended Application
Lightweight aggregates
Concrete and cement
Bricks and tiles
Previous applications
Road construction
Dike
Background and study objectives

## Slide 7
What is a sealing asphalt ?
Background and study objectives
7
Bitumen
LS Filler
Porphyry
Sand
Composition
Benefit
Ecological
Punctual repairs
Appearance and special aspect
None voids
Waterproof
Self compacting
42% by mass
Durability

## Slide 8
Background and study objectives
8
Bridge
Industrial soil
Road
Parking
Tank
Reparation
Bicycle path
Walkways
Applications of sealing asphalt

## Slide 9
Valorisation of mineral wastes in asphalt materials
Powder of glass
Powder of bricks
Fly ash
Rice husk ash
Powder of marble
sawdust
Powder of ceramic
Background and study objectives
9

## Slide 10
Bitume
Filler
Porphyre
Sable
Valorisation of mineral wastes in asphalt materials
Background and study objectives
10
Raw sediments
Pretreatment
Mix optimization
Physical
Grinding
Chemical
CaO
Thermal
Flash Calcination

## Slide 11
Materials and research methodology
11
Sediments were collected from different rivers on the north of France
Noyelles-sous-Lens (NSL)
Aire-sur-la-Lys (ASL)
European Metropolis of Lille (MEL)
Urban Community of Arras (ARS)
Homogenization and subsampling
Materials

## Slide 12
Thermal
Flash Calcination
12
Materials and research methodology
Pre-treatment of the sediments
Ishai and Craus (1977).
Spherical form
Time :
2 à 3 secs

## Slide 13
Materials and research methodology
13
Environmental characterisation
Paramètre | Unité | Inert | Non hazardous |  | CU-Arras | ASL | MEL | NSL
matière sèche | % massique | <30 |  |  | 67,3 | 85,6 | 95,6 | 65,6
TOC | mg/kg MS | 30 000 | 50 000 |  | 37 200 | 27 000 | 73 000 | 90 000
BTEX | mg/kg MS | 6 | 30 |  | 0,25 | 0,3 | 0,25 | 2
PAH (16) - EPA | mg/kg MS | 50 | 100 |  | 4,4 | 2,87 | 46 | 22
PCB totaux (7) | Mg/kg MS | 1 | 50 |  | 0,013 | 0,05 | 46 | 0,26
Hydrocarbures totaux C10-C40 | mg/kg MS | 500 | 5000 |  | 427 | 1,3 | 505 | 2320
Métaux lourds sur éluats en (mg/kg de matière sèche ) |  |  |  |  |  |  |  | 
antimoine | mg/kg MS | 0,06 | 0,7 | - |  | <0,03 | 0,14 | 0,09
arsenic | mg/kg MS | 0,5 | 2 | <0,04 |  | 0,34 | 0,05 | <0,05
baryum | mg/kg MS | 20 | 100 | 1,04 |  | 0,35 | 0,35 | 0,43
cadmium | mg/kg MS | 0,04 | 1 | 0,01 |  | 0,01 | 0,004 | 0,01
chrome | mg/kg MS | 0,5 | 10 | 0,02 |  | 0,365 | 0,012 | <0,01
cuivre | mg/kg MS | 2 | 50 | <0,05 |  | 0,37 | 0,4 | 0,28
mercure | mg/kg MS | 0,01 | 0,2 | <0,0005 |  | 0,11 | 0,01 | <0,01
plomb | mg/kg MS | 0,5 | 10 | <0,1 |  | 0,49 | 0,1 | <0,1
molybdène | mg/kg MS | 0,5 | 10 | 0,05 |  | 0,049 | 0,063 | 0,11
nickel | mg/kg MS | 0,4 | 10 | 0,02 |  | 0,16 | 0,1 | 0,13
sélénium | mg/kg MS | 0,1 | 0,5 | <0,039 |  | 0,022 | 0,039 | 0,05
zinc | mg/kg MS | 4 | 50 | 0,09 |  | 1,85 | 0,21 | 1,2
Autre paramètre sur éluats |  |  |  |  |  |  |  | 
TOC | mg/kg MS | 500 | 800 | 82 |  | 47 | 94 | 94
Indice phénol | mg/kg MS | 1 | 10 | <0,1 |  | - | <0,1 | <0,1
chlorures | mg/kg MS | 800 | 15000 | 42 |  | 55,46 | 24 | 20
sulfate | mg/kg MS | 1000 | 20 000 | 930 |  | 552,3 | 554 | 5350
The ASL sediments was classified as Inert waste
ARS, MEL and NSL sediments were considered as Non-hazardous non-inert waste

## Slide 14
Materials and research methodology
14
Oxyde | NSL | ASL | ARS | MEL | LS
Al2O3 | 13,42 | 11,9 | 10,96 | 11,15 | 0.14
SiO2 | 37,01 | 59,26 | 59,68 | 51,98 | 0.47
CaO | 19,87 | 9,51 | 9,65 | 13,29 | 98,33
Mineralogical characterisation
The sediments are composed mainly of quartz (SiO2) and calcite (CaCO3)

## Slide 15
Materials and research methodology
15
Specifications
Glass of Bitumen - Penetration NF EN 1426 1/10 mm ≥ 35
Bitumen after extraction 16 - 22 %
Fines after extraction ≥ 45%
Indentation NF EN 12697fabricationtype a :70 ≤ i ≤ 100
Maximal temperature of fabrication : ≤ 200 °c

## Slide 16
Materials and research methodology
16
Mix design (Design-Expert software)
Comp. | Name | Units | Type | Minimum | Maximum
A | Bitumen | % | Mixture | 0.18 | 0.22
B | LS Filler | % | Mixture | 0.294 | 0.42
C | sediment | % | Mixture | 0 | 0.126
D | sable | % | Mixture | 0.4 | 0.4
 |  |  |  | Total = | 1.00
controle | Bitumen (%) | Filler(%) | Sediment(%) | Sand(%)
R2 | 18 | 42 | 0 | 40
R1 | 20 | 40 | 0 | 40
R3 | 22 | 38 | 0 | 40
Mélange | Bitumen (%) | LS Filler(%) | Sediment (%) | Sed/Filler total (%) | Sand (%)
M1 | 18 | 35,7 | 6,3 | 15 | 40
M2 | 18 | 29,4 | 12,6 | 30 | 40
M3 | 18 | 37,8 | 4,2 | 10 | 40
M4 | 22 | 29,4 | 8,6 | 23 | 40
M5 | 21 | 32,05 | 6,95 | 18 | 40
M6 | 20 | 36,47 | 2,87 | 7 | 40
M7 | 20 | 29,4 | 10,6 | 27 | 40
M8 | 22 | 33,7 | 4,3 | 11 | 40

## Slide 17
Results
17
Indentation results of the asphalt based on raw sediments
Two mixtures that are admissible M4 & M8 with a single sediment (ASL), and M8 mixture is admissible for all sediments.
The higher the sediment content in the matrix, induce the decrease on the indentation
The amount of bitumen used is of the order of 22%

## Slide 18
Results
18
A slight increase in indentation for mixtures based on quicklime-treated sediments
The better mixture were ASLT and ARST
The amount of sediment requires increase the demand for bitumen
Organic matter is the main factor of the low indentation
Indentation results of the asphalt based on treated sediments with CaO

## Slide 19
Results
19
ASL
ASL.T
2D Illustration of the indentations of asphalt based on raw sediments and treated sediments with CaO

## Slide 20
Results
20
Illustration of the indentations of asphalt based on calcined sediments and treated sediments with CaO
The flash calcination improve the indentation compared with the value of SED C.
The increase in indentation can be up to 60% with flash calcined sediments

## Slide 21
Results
21
Model of regression
Regression Model of Scheffé
Y: predicted solution
q : number of constituents (ici, q=3: cement, ggbs and addition); βiet βij: coefficients of model;
Xi: proportions of constituants.
Sédiment | β1 | β2 | β3 | β12 | β13 | β23
ASL | +3927.02626 | +401.44792 | +1535.90061 | -10918.69439 | -13705.65040 | -2660.45649
ARS | +5730.54278 | +856.87995 | +2385.86243 | -17727.56530 | -23173.60494 | -2709.29682
MEL | +6011.71690 | +910.81042 | +3186.24946 | -18706.23771 | -26317.20961 | -3927.36654
NSL | +7027.17467 | +1209.20670 | +3790.57894 | -22754.47090 | -30542.84550 | -4919.95349
ASLT | +4396.77668 | +507.59401 | +1104.64448 | -12624.63511 | -13942.62581 | -1701.68626
ARST | +4449.12579 | +495.10303 | +1197.42436 | -12690.77060 | -15954.07461 | -1175.49932
MELT | +5553.89236 | +806.15951 | +2463.74858 | -17033.05036 | -22522.71762 | -3104.04632
NSLT | +10595.33790 | +2379.06126 | +3891.56407 | -37469.85487 | -37636.93804 | -6477.21395
MELC | +7389.27423 | +1204.84591 | +1938.51297 | -23622.19939 | -25787.90233 | -1781.86374
NSLC | +8421.79956 | +1471.04600 | +2814.41061 | -27548.00157 | -31770.52182 | -2728.01978
ASLB | -4165.36017 | -1157.71808 | -2030.46879 | +17544.79860 | +26224.13580 | -3718.63034
ASLTB | -4015.54348 | -1170.25230 | -1514.50416 | +17247.13691 | +20793.89736 | -1879.90732
Coefficients of the model for different sediments
Prediction model

## Slide 22
Results
22
Sediment | Av; Indentation predict (1/10)mm | 95% confidence (1/10)mm | Av. Experimental Indentation (1/10)mm
ASL | 75.68 | [73.24-79.89] | 73.14
ARS | 69.47 | [64.45-73.85] | 65.75
MEL | 64.01 | [59.43-70.12] | 60.98
NSL | 59.22 | [53.16-66.22] | 55.17
ASLT | 80.01 | [77.32-83.11] | 81.55
ARST | 77.10 | [74.37-88.45] | 75.42
MELT | 68.70 | [63.52-73.25] | 64.87
NSLT | 60.19 | [54.71-65.12] | 57.57
MELC | 78.29 | [74.61-82.23] | 77.26
NSLC | 72.81 | [67.32-77.36] | 69.14
ASLB | 99.31 | [92.89-99.27] | 100.03
ASLTB | 104.87 | [101.43-108.31] | 107.14
Validation of the model
Mix based on 3,15% sediment (8% substitution de filler )
35,7 % filler 21,15% bitumen 40% sand
Average of the indentation values within the 95 % confidence interval
All models are validated, Indentation predictions with high accuracy

## Slide 23
Results
23
Bitumen absorption is more important for filler sediments
A slight improvement/decrease in this absorption of lime-treated sediments
A significant decrease in the absorption of calcined sediments
Interpretation

## Slide 24
Results
24
A strong correlation between indentation and organic matter R2=84%
A strong correlation between indentation and inter-granular porosity (RV)
Correlation indentation VS Rigden Voids
Correlation indentation VS organic matter

## Slide 25
Conclusions and perspectives
25
The flash calcination improves the quality of fillers from waste
The lime-treatement sediments have a slight improvement
A softer bitumen grade can give satisfactory results
The IA can be use to predict the indentation values
https://www.sedilab.com/portfolio-item/sediasphalte/
Web site

## Slide 26
Thank you for your attention !!
Walid MAHERZI
walid.maherzi@imt-nord-europe.fr
@WalidMAHERZI
Assistant professor at IMT Nord Europe,
France
26
logos
Notes: Thank you everyone and i will be happy to take questions